SECTION 02921

- TOPSOIL

PART 1 - GENERAL

## SUMMARY

#### This work shall consist of excavating, or removing from stockpiles, hauling, depositing, and spreading topsoil.

PART 2 – PRODUCTS

## SOURCE

#### Topsoil shall be obtained from all site and structural excavation.

## QUALITY

#### Topsoil shall consist of loose, friable, sandy loam, free of admixture of subsoil, refuse, stumps, roots, rocks, brush, weeds, or other material that would be detrimental to the development of vegetative growth.  Topsoil, as used herein, shall mean that portion of the soil profile defined technically as the "A" horizon by the Soil Science Society of America.

#### Topsoil shall have a grading analysis as follows:

| Sieve Designation | Percentage by Weight Mesh Sieve | Passing Square |
| --- | --- | --- |
| 1" | 100 |  |
| 1/4" | 97-100 |  |
| No. 10 | 80-100 |  |

#### The minimum and maximum pH values shall be 5 and 8, respectively.

#### Topsoil shall contain a minimum of 3 percent and a maximum of 20 percent organic matter as determined by loss on ignition of samples oven dried to constant weight at 212 F.

#### Topsoil shall consist of the following particle sizes:

| Material | Size | Percent in Topsoil Min. Max |  |
| --- | --- | --- | --- |
| Sand | 0.075-2 mm. | 20 | 75 |
| Silt | 0.002-0.075 mm. | 1030 |  |
| Clay | 0.002 mm. Or less | 5 | 30 |

#### Prior to stripping, topsoil shall have demonstrated by the occurrence upon it of healthy crops, grass, or other plant growth, that it is of good quality and reasonably free draining.

PART 3 – EXECUTION

## SPREADING

#### The topsoil shall be deposited and spread to the depth and at the locations SHOWN ON THE DRAWINGS.

#### Topsoil shall not be spread when the ground or topsoil is frozen, excessively wet, or in a condition detrimental to the work.

#### Large clods, rocks larger than 2 inches in any dimension, roots, stumps, and other litter shall be removed, and disposed of at the designated waste area.

## HAULING

#### The roadbed surfacing shall be kept clean during hauling operations.  Topsoil or other soil deposited upon the surfacing shall be removed before it becomes compacted by traffic.

END OF SECTION 02921