SECTION 055213

PIPE AND TUBE RAILINGS

- GENERAL

      - RELATED DOCUMENTS

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

      - SUMMARY

        - This Section includes the following:

Adjust list below to suit Project.

          - Steel pipe railings.

        - Related Sections include the following:

          - Division 05 Section "Metal Stairs" for steel tube railings associated with metal stairs.

      - PERFORMANCE REQUIREMENTS

        - General:  In engineering railings to withstand structural loads indicated, determine allowable design working stresses of railing materials based on the following:

          - Steel:  80 percent of minimum yield strength.

        - Structural Performance:  Provide railings capable of withstanding the effects of gravity loads and the following loads and stresses within limits and under conditions indicated:

          - Handrails:

            - Concentrated load of 200 lbf (0.89 kN) applied in any direction.

            - Uniform and concentrated loads need not be assumed to act concurrently.

          - Infill of Guards:

            - Concentrated load of 200 lbf (0.89 kN)] applied horizontally.

            - Infill load and other loads need not be assumed to act concurrently.

        - Thermal Movements:  Provide exterior railings that allow for thermal movements resulting from the following maximum change (range) in ambient and surface temperatures by preventing buckling, opening of joints, overstressing of components, failure of connections, and other detrimental effects.  Base engineering calculation on surface temperatures of materials due to both solar heat gain and nighttime-sky heat loss.

          - Temperature Change (Range):  120 deg F (67 deg C), ambient; 180 deg F (100 deg C), material surfaces.

        - Control of Corrosion:  Prevent galvanic action and other forms of corrosion by insulating metals and other materials from direct contact with incompatible materials.

      - SUBMITTALS

        - Product Data:  For the following:

          - Manufacturer's product lines of mechanically connected railings.

          - Grout, anchoring cement, and paint products.

        - Shop Drawings:  Include plans, elevations, sections, details, and attachments to other work.

          - For installed products indicated to comply with design loads, include structural analysis data signed and sealed by the qualified professional engineer responsible for their preparation.

        - Welding certificates.

        - Product Test Reports:  Based on evaluation of comprehensive tests performed by a qualified testing agency, according to ASTM E 894 and ASTM E 935.

      - QUALITY ASSURANCE

        - Source Limitations:  Obtain each type of railing through one source from a single manufacturer.

        - Welding:  Qualify procedures and personnel according to the following:

          - AWS D1.1, "Structural Welding Code--Steel."

      - PROJECT CONDITIONS

        - Field Measurements:  Verify actual locations of other construction contiguous with railings by field measurements before fabrication and indicate measurements on Shop Drawings.

          - Established Dimensions:  Where field measurements cannot be made without delaying the Work, establish dimensions and proceed with fabricating railings without field measurements.  Coordinate other contiguous construction to ensure that actual dimensions correspond to established dimensions.

          - Provide allowance for trimming and fitting at site.

      - COORDINATION AND SCHEDULING

        - Coordinate installation of anchorages for railings.  Furnish setting drawings, templates, and directions for installing anchorages.  Deliver such items to Project site in time for installation.

        - Schedule installation so attachments are made only to completed construction.  Do not support railings temporarily by any means that do not satisfy structural performance requirements.

- PRODUCTS

      - MANUFACTURERS

        - Available Manufacturers:  Subject to compliance with requirements, manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following:

        - Manufacturers:  Subject to compliance with requirements, provide products by one of the following:

          - Steel Pipe and Tube Railings:

            - Pisor Industries, Inc.

            - Sharpe Products.

            - Wagner, R & B, Inc.; a division of the Wagner Companies.

      - METALS, GENERAL

        - Metal Surfaces, General:  Provide materials with smooth surfaces, without seam marks, roller marks, rolled trade names, stains, discolorations, or blemishes.

        - Brackets, Flanges, and Anchors:  Cast or formed metal of same type of material and finish as supported rails, unless otherwise indicated.

      - STEEL

        - Tubing:  ASTM A 847.

        - Plates, Shapes, and Bars:  ASTM A 588/A 588M.

      - FASTENERS

        - General:  Provide the following:

          - Steel Railings:  ASTM A325 Weathering Steel.

        - Fasteners for Anchoring Railings to Other Construction:  Select fasteners of type, grade, and class required to produce connections suitable for anchoring railings to other types of construction indicated and capable of withstanding design loads.

        - Fasteners for Interconnecting Railing Components:

          - Provide concealed fasteners for interconnecting railing components and for attaching them to other work, unless otherwise indicated.

          - Provide Phillips flat-head machine screws for exposed fasteners, unless otherwise indicated.

      - MISCELLANEOUS MATERIALS

        - Welding Rods and Bare Electrodes:  Select according to AWS specifications for metal alloy welded.

          - For aluminum railings, provide type and alloy as recommended by producer of metal to be welded and as required for color match, strength, and compatibility in fabricated items.

        - Nonshrink, Nonmetallic Grout:  Factory-packaged, nonstaining, noncorrosive, nongaseous grout complying with ASTM C 1107.  Provide grout specifically recommended by manufacturer for interior and exterior applications.

      - FABRICATION

        - General:  Fabricate railings to comply with requirements indicated for design, dimensions, member sizes and spacing, details, finish, and anchorage, but not less than that required to support structural loads.

        - Assemble railings in the shop to greatest extent possible to minimize field splicing and assembly.  Disassemble units only as necessary for shipping and handling limitations.  Clearly mark units for reassembly and coordinated installation.  Use connections that maintain structural value of joined pieces.

        - Cut, drill, and punch metals cleanly and accurately.  Remove burrs and ease edges to a radius of approximately 1/32 inch (1 mm), unless otherwise indicated.  Remove sharp or rough areas on exposed surfaces.

        - Form work true to line and level with accurate angles and surfaces.

        - Fabricate connections that will be exposed to weather in a manner to exclude water.  Provide weep holes where water may accumulate.

        - Cut, reinforce, drill, and tap as indicated to receive finish hardware, screws, and similar items.

        - Connections:  Fabricate railings with welded connections, unless otherwise indicated.

        - Welded Connections:  Cope components at connections to provide close fit, or use fittings designed for this purpose.  Weld all around at connections, including at fittings.

          - Use materials and methods that minimize distortion and develop strength and corrosion resistance of base metals.

          - Obtain fusion without undercut or overlap.

          - Remove flux immediately.

          - At exposed connections, finish exposed surfaces smooth and blended so no roughness shows after finishing and welded surface matches contours of adjoining surfaces.

        - Nonwelded Connections:  Connect members with concealed mechanical fasteners and fittings.  Fabricate members and fittings to produce flush, smooth, rigid, hairline joints.

        - Form changes in direction as follows:

          - By radius bends or by inserting prefabricated elbow fittings of radius indicated.

        - Form simple and compound curves by bending members in jigs to produce uniform curvature for each repetitive configuration required; maintain cross section of member throughout entire bend without buckling, twisting, cracking, or otherwise deforming exposed surfaces of components.

        - Close exposed ends of railing members with prefabricated end fittings.

        - Brackets, Flanges, Fittings, and Anchors:  Provide wall brackets, flanges, miscellaneous fittings, and anchors to interconnect railing members to other work, unless otherwise indicated.

        - Toe Boards:  Where indicated, provide toe boards at railings around openings and at edge of open-sided floors and platforms.  Fabricate to dimensions and details indicated.

- EXECUTION

      - INSTALLATION, GENERAL

        - Fit exposed connections together to form tight, hairline joints.

        - Perform cutting, drilling, and fitting required for installing railings.  Set railings accurately in location, alignment, and elevation; measured from established lines and levels and free of rack.

          - Do not weld, cut, or abrade surfaces of railing components that have been coated or finished after fabrication and that are intended for field connection by mechanical or other means without further cutting or fitting.

          - Set posts plumb within a tolerance of 1/16 inch in 3 feet (2 mm in 1 m).

          - Align rails so variations from level for horizontal members and variations from parallel with rake of steps and ramps for sloping members do not exceed 1/4 inch in 12 feet (5 mm in 3 m).

        - Adjust railings before anchoring to ensure matching alignment at abutting joints.

        - Fastening to In-Place Construction:  Use anchorage devices and fasteners where necessary for securing railings and for properly transferring loads to in-place construction.

      - RAILING CONNECTIONS

        - Nonwelded Connections:  Use mechanical joints for permanently connecting railing components.

        - Welded Connections:  Use fully welded joints, where indicated, for permanently connecting railing components.  Comply with requirements for welded connections in Part 2 "Fabrication" Article whether welding is performed in the shop or in the field.

        - Expansion Joints:  Install expansion joints at locations indicated but not farther apart than required to accommodate thermal movement.  Provide slip-joint internal sleeve extending 2 inches (50 mm) beyond joint on either side, fasten internal sleeve securely to 1 side, and locate joint within 6 inches (150 mm) of post.

      - ANCHORING POSTS

        - Anchor posts to metal surfaces with oval flanges, angle type, or floor type as required by conditions, connected to posts and to metal supporting members as follows:

          - For steel pipe railings, weld flanges to post and bolt to metal supporting surfaces.

      - ANCHORING RAILING ENDS

        - Anchor railing ends to concrete and masonry with round flanges connected to railing ends and anchored to wall construction with anchors and bolts.

        - Anchor railing ends to metal surfaces with flanges bolted to metal surfaces and welded to railing ends or connected to railing ends using nonwelded connections.

END OF SECTION 055213