SECTION 055000

METAL FABRICATIONS

      - RELATED DOCUMENTS

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

      - SUMMARY

        - This Section includes the following:

          - Steel framing and supports for applications where framing and supports are not specified in other Sections.

        - Products furnished, but not installed, under this Section include the following:

          - Anchor rods, steel pipe sleeves, and wedge-type inserts indicated to be cast into concrete or built into unit masonry.

        - Related Sections include the following:

          - Division 03 Section "Cast-in-Place Concrete" for installing anchor bolts and other items indicated to be cast into concrete.

          - Division 05 Section "Structural Steel Framing."

          - Division 05 Section "Metal Stairs."

          - Division 05 Section "Metal Gratings."

      - PERFORMANCE REQUIREMENTS

        - Thermal Movements:  Provide exterior metal fabrications that allow for thermal movements resulting from the following maximum change (range) in ambient and surface temperatures by preventing buckling, opening of joints, overstressing of components, failure of connections, and other detrimental effects.  Base engineering calculation on surface temperatures of materials due to both solar heat gain and nighttime-sky heat loss.

          - Temperature Change (Range):  120 deg F (67 deg C), ambient; 180 deg F (100 deg C), material surfaces.

      - SUBMITTALS

        - Product Data:  For the following:

          - Paint products.

          - Grout.

        - Shop Drawings:  Show fabrication and installation details for metal fabrications.

          - Include plans, elevations, sections, and details of metal fabrications and their connections.  Show anchorage and accessory items.

          - Provide templates for anchors and bolts specified for installation under other Sections.

        - Welding certificates.

      - QUALITY ASSURANCE

        - Welding:  Qualify procedures and personnel according to the following:

          - AWS D1.1, "Structural Welding Code--Steel."

          - AWS D1.3, "Structural Welding Code--Sheet Steel."

      - PROJECT CONDITIONS

        - Field Measurements:  Verify actual locations of walls and other construction contiguous with metal fabrications by field measurements before fabrication and indicate measurements on Shop Drawings.

          - Established Dimensions:  Where field measurements cannot be made without delaying the Work, establish dimensions and proceed with fabricating metal fabrications without field measurements.  Coordinate with other contiguous construction to ensure that actual dimensions correspond to established dimensions.

          - Provide allowance for trimming and fitting at site.

      - COORDINATION

        - Coordinate installation of anchorages for metal fabrications.  Furnish setting drawings, templates, and directions for installing anchorages, including sleeves, concrete inserts, anchor bolts, and items with integral anchors, that are to be embedded in concrete or masonry.  Deliver such items to Project site in time for installation.

        - Coordinate installation of steel weld plates and angles for casting into concrete that are specified in this Section but required for work of another Section.  Deliver such items to Project site in time for installation.

- PRODUCTS

      - MANUFACTURERS

        - In other Part 2 articles where titles below introduce lists, the following requirements apply to product selection:

          - Available Products:  Subject to compliance with requirements, products that may be incorporated into the Work include, but are not limited to, products specified.

          - Available Manufacturers:  Subject to compliance with requirements, manufacturers offering products that may be incorporated into the Work include, but are not limited to, manufacturers specified.

      - METALS, GENERAL

        - Metal Surfaces, General:  Provide materials with smooth, flat surfaces, unless otherwise indicated.  For metal fabrications exposed to view in the completed Work, provide materials without seam marks, roller marks, rolled trade names, or blemishes.

      - FERROUS METALS

        - Steel Plates, Shapes, and Bars to be painted:  ASTM A 36/A 36M.

        - Corrosion Resistant Steel Plates, Shapes and Bars: ASTM A588/A588M

        - Steel Tubing:  ASTM A 500 Grade B, cold-formed steel tubing.

        - Steel Pipe:  ASTM A 53/A 53M, standard weight (Schedule 40), unless another weight is indicated or required by structural loads.

      - FASTENERS

        - Steel Bolts and Nuts:  Regular hexagon-head bolts, ASTM A 307, Grade A (ASTM F 568M, Property Class 4.6); with hex nuts, ASTM A 563 (ASTM A 563M); and, where indicated, flat washers with hot dipped galvanized finish.

        - Anchor Rods:  ASTM F 1554, Grade 36.

          - Provide hot-dip or mechanically deposited, zinc-coated anchor bolts where item being fastened is indicated to be galvanized.

        - Eyebolts:  ASTM A 489.

        - Machine Screws:  ASME B18.6.3 (ASME B18.6.7M).

        - Plain Washers:  Round, ASME B18.22.1 (ASME B18.22M).

        - Lock Washers:  Helical, spring type, ASME B18.21.1 (ASME B18.21.2M).

        - Cast-in-Place Anchors in Concrete:  Anchors capable of sustaining, without failure, a load equal to four times the load imposed, as determined by testing according to ASTM E 488, conducted by a qualified independent testing agency.

          - Threaded or wedge type; galvanized ferrous castings, either ASTM A 47/A 47M malleable iron or ASTM A 27/A 27M cast steel.  Provide bolts, washers, and shims as needed, hot-dip galvanized per ASTM A 153/A 153M.

        - Expansion Anchors:  Anchor bolt and sleeve assembly with capability to sustain, without failure, a load equal to six times the load imposed when installed in unit masonry and four times the load imposed when installed in concrete, as determined by testing according to ASTM E 488, conducted by a qualified independent testing agency.

          - Material for Anchors in Interior Locations:  Carbon-steel components zinc-plated to comply with ASTM B 633, Class Fe/Zn 5.

          - Material for Anchors in Exterior Locations:  Alloy Group 1 (A1) stainless-steel bolts complying with ASTM F 593 (ASTM F 738M) and nuts complying with ASTM F 594 (ASTM F 836M).

      - MISCELLANEOUS MATERIALS

        - Welding Rods and Bare Electrodes:  Select according to AWS specifications for metal alloy welded.

        - Zinc-Rich Primer:  Complying with SSPC-Paint 20 or SSPC-Paint 29 and compatible with topcoat.

          - Use primer with a VOC content of 420 g/L (3.5 lb/gal.) or less when calculated according to 40 CFR 59, Subpart D (EPA Method 24).

          - Available Products:

            - Benjamin Moore & Co.; Epoxy Zinc-Rich Primer CM18/19.

            - Carboline Company; Carbozinc 621.

            - ICI Devoe Coatings; Catha-Coat 313.

            - International Coatings Limited; Interzinc 315 Epoxy Zinc-Rich Primer.

            - PPG Architectural Finishes, Inc.; Aquapon Zinc-Rich Primer 97-670.

            - Sherwin-Williams Company (The); Corothane I GalvaPac Zinc Primer.

            - Tnemec Company, Inc.; Tneme-Zinc 90-97.

        - Galvanizing Repair Paint:  High-zinc-dust-content paint for regalvanizing welds in steel, complying with SSPC-Paint 20.

        - Bituminous Paint:  Cold-applied asphalt emulsion complying with ASTM D 1187.

        - Nonshrink, Nonmetallic Grout:  Factory-packaged, nonstaining, noncorrosive, nongaseous grout complying with ASTM C 1107.  Provide grout specifically recommended by manufacturer for interior and exterior applications.

      - FABRICATION, GENERAL

        - Shop Assembly:  Preassemble items in the shop to greatest extent possible.  Disassemble units only as necessary for shipping and handling limitations.  Use connections that maintain structural value of joined pieces.  Clearly mark units for reassembly and coordinated installation.

        - Cut, drill, and punch metals cleanly and accurately.  Remove burrs and ease edges to a radius of approximately 1/32 inch (1 mm), unless otherwise indicated.  Remove sharp or rough areas on exposed surfaces.

        - Form bent-metal corners to smallest radius possible without causing grain separation or otherwise impairing work.

        - Form exposed work true to line and level with accurate angles and surfaces and straight edges.

        - Weld corners and seams continuously to comply with the following:

          - Use materials and methods that minimize distortion and develop strength and corrosion resistance of base metals.

          - Obtain fusion without undercut or overlap.

          - Remove welding flux immediately.

          - At exposed connections, finish exposed welds and surfaces smooth and blended so no roughness shows after finishing and contour of welded surface matches that of adjacent surface.

        - Form exposed connections with hairline joints, flush and smooth, using concealed fasteners where possible.  Where exposed fasteners are required, use Phillips flat-head (countersunk) screws or bolts, unless otherwise indicated.  Locate joints where least conspicuous.

        - Fabricate seams and other connections that will be exposed to weather in a manner to exclude water.  Provide weep holes where water may accumulate.

        - Cut, reinforce, drill, and tap metal fabrications as indicated to receive finish hardware, screws, and similar items.

        - Provide for anchorage of type indicated; coordinate with supporting structure.  Space anchoring devices to secure metal fabrications rigidly in place and to support indicated loads.

      - MISCELLANEOUS FRAMING AND SUPPORTS

        - General:  Provide steel framing and supports not specified in other Sections as needed to complete the Work.

        - Fabricate units from steel shapes, plates, and bars of welded construction of material types compatible with supporting structural steel, unless otherwise indicated.  Fabricate to sizes, shapes, and profiles indicated and as necessary to receive adjacent construction retained by framing and supports.  Cut, drill, and tap units to receive hardware, hangers, and similar items.

          - Furnish inserts if units are installed after concrete is placed.

        - Galvanize miscellaneous framing and supports where indicated.

        - Prime miscellaneous framing and supports with zinc-rich primer where indicated.

      - LOOSE BEARING AND LEVELING PLATES

        - Provide loose bearing and leveling plates for steel items bearing on concrete construction.  Drill plates to receive anchor bolts and for grouting.

        - Galvanize plates after fabrication.

      - STEEL WELD PLATES AND ANGLES

        - Provide steel weld plates and angles not specified in other Sections, for items supported from concrete construction as needed to complete the Work.  Provide each unit with not less than two integrally welded steel strap anchors for embedding in concrete.

      - MISCELLANEOUS STEEL TRIM

        - Unless otherwise indicated, fabricate units from steel shapes, plates, and bars of profiles shown with continuously welded joints and smooth exposed edges.  Use steel material types consistent Miter corners and use concealed field splices where possible.

        - Provide cutouts, fittings, and anchorages as needed to coordinate assembly and installation with other work.

          - Provide with integrally welded steel strap anchors for embedding in concrete or masonry construction.

        - Galvanize exterior miscellaneous steel trim where indicated.

        - Prime exterior miscellaneous steel trim with zinc-rich primer.

      - FINISHES, GENERAL

        - Comply with NAAMM's "Metal Finishes Manual for Architectural and Metal Products" for recommendations for applying and designating finishes.

        - Finish metal fabrications after assembly.

      - STEEL AND IRON FINISHES

        - Galvanizing:  Hot-dip galvanize items as indicated to comply with applicable standard listed below:

          - ASTM A 153/A 153M, for galvanizing steel and iron hardware.

        - Preparation for Shop Priming:  Prepare uncoated ferrous-metal surfaces to comply with minimum requirements indicated below for SSPC surface preparation specifications and environmental exposure conditions of installed metal fabrications:

          - Exteriors (SSPC Zone 1B) and Items Indicated to Receive Zinc-Rich Primer:  SSPC-SP 6/NACE No. 3, "Commercial Blast Cleaning."

        - Shop Priming:  Apply shop primer to uncoated surfaces of metal fabrications, except those with galvanized finishes and those to be embedded in concrete unless otherwise indicated.  Comply with SSPC-PA 1, "Paint Application Specification No. 1: Shop, Field, and Maintenance Painting of Steel," for shop painting.

          - Stripe paint corners, crevices, bolts, welds, and sharp edges.

- EXECUTION

      - INSTALLATION, GENERAL

        - Cutting, Fitting, and Placement:  Perform cutting, drilling, and fitting required for installing metal fabrications.  Set metal fabrications accurately in location, alignment, and elevation; with edges and surfaces level, plumb, true, and free of rack; and measured from established lines and levels.

        - Fit exposed connections accurately together to form hairline joints.  Weld connections that are not to be left as exposed joints but cannot be shop welded because of shipping size limitations.  Do not weld, cut, or abrade surfaces of exterior units that have been hot-dip galvanized after fabrication and are for bolted or screwed field connections.

        - Field Welding:  Comply with the following requirements:

          - Use materials and methods that minimize distortion and develop strength and corrosion resistance of base metals.

          - Obtain fusion without undercut or overlap.

          - Remove welding flux immediately.

          - At exposed connections, finish exposed welds and surfaces smooth and blended so no roughness shows after finishing and contour of welded surface matches that of adjacent surface.

        - Fastening to In-Place Construction:  Provide anchorage devices and fasteners where metal fabrications are required to be fastened to in-place construction.

        - Provide temporary bracing or anchors in formwork for items that are to be built into concrete, masonry, or similar construction.

      - INSTALLING MISCELLANEOUS FRAMING AND SUPPORTS

        - General:  Install miscellaneous framing and supports to comply with requirements of items being supported, including manufacturers' written instructions and requirements indicated on Shop Drawings.

      - INSTALLING BEARING AND LEVELING PLATES

        - Clean concrete bearing surfaces of bond-reducing materials, and roughen to improve bond to surfaces.  Clean bottom surface of plates.

        - Set bearing and leveling plates on wedges, shims, or leveling nuts.  After bearing members have been positioned and plumbed, tighten anchor bolts.  Do not remove wedges or shims but, if protruding, cut off flush with edge of bearing plate before packing with grout.

          - Use nonshrink, nonmetallic grout unless otherwise indicated.

          - Pack grout solidly between bearing surfaces and plates to ensure that no voids remain.

      - ADJUSTING AND CLEANING

        - Touchup Painting:  Cleaning and touchup painting of field welds, bolted connections, and abraded areas of shop paint are specified in Division 09 painting Sections.

        - Galvanized Surfaces:  Clean field welds, bolted connections, and abraded areas and repair galvanizing to comply with ASTM A 780.

END OF SECTION 055000