SECTION 05530

METAL GRATINGS

- GENERAL

      - RELATED DOCUMENTS

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

      - SUMMARY

        - This Section includes the following:

          - Metal bar gratings.

          - Metal frames and supports for gratings.

        - Related Sections include the following:

          - Division 05 Section "Structural Steel Framing" for structural-steel framing system components.

          - Division 05 Section "Metal Stairs" for grating treads and landings of steel-framed stairs.

          - Division 05 Section "Pipe and Tube Railings" for metal pipe and tube handrails and railings.

      - PERFORMANCE REQUIREMENTS

        - Structural Performance of Gratings:  Provide gratings capable of withstanding the effects of gravity loads and the following loads and stresses within limits and under conditions indicated:

          - Floors:  Uniform load of 100 lbf/sq. ft. (4.78 kN/sq. m) or concentrated load of 1000 lbf (4.45 kN), whichever produces the greater stress.

        - Seismic Performance:  Provide gratings capable of withstanding the effects of earthquake motions determined according to ASCE 7, "Minimum Design Loads for Buildings and Other Structures":  Section 9, "Earthquake Loads."

      - SUBMITTALS

        - Product Data:  For the following:

          - Rectangular Bar Steel grating.

        - Shop Drawings:  Include plans, elevations, sections, details, and attachments to other work.

          - Provide templates for anchors and bolts specified for installation under other Sections.

          - For installed products indicated to comply with design loads, include structural analysis data signed and sealed by the qualified professional engineer responsible for their preparation.

        - Mill Certificates:  Signed by manufacturers of stainless-steel sheet certifying that products furnished comply with requirements.

        - Welding certificates.

        - Qualification Data:  For professional engineer.

      - QUALITY ASSURANCE

        - Metal Bar Grating Standards:  Comply with NAAMM MBG 531, "Metal Bar Grating Manual."

        - Welding:  Qualify procedures and personnel according to the following:

          - AWS D1.1, "Structural Welding Code--Steel."

      - PROJECT CONDITIONS

        - Field Measurements:  Verify actual locations of walls and other construction contiguous with gratings by field measurements before fabrication and indicate measurements on Shop Drawings.

          - Established Dimensions:  Where field measurements cannot be made without delaying the Work, establish dimensions and proceed with fabricating gratings without field measurements.  Coordinate wall and other contiguous construction to ensure that actual dimensions correspond to established dimensions.

          - Provide allowance for trimming and fitting at site.

      - COORDINATION

        - Coordinate installation of anchorages for gratings, grating frames, and supports.  Furnish setting drawings, templates, and directions for installing anchorages, including sleeves, concrete inserts, anchor bolts, and items with integral anchors, that are to be embedded in concrete or masonry.  Deliver such items to Project site in time for installation.

- PRODUCTS

      - MANUFACTURERS

        - Available Manufacturers:  Subject to compliance with requirements, manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following:

          - Metal Bar Gratings:

            - Alabama Metal Industries Corporation.

            - All American Grating, Inc.

            - Barnett/Bates Corp.

            - Borden Metal Products (Canada) Limited.

            - Fisher & Ludlow.

            - Grupo Metelmex, S.A. de C.V.

            - IKG Industries; a Harsco Company.

            - Marwas Steel Co.; Laurel Steel Products Division.

            - Ohio Gratings, Inc.

            - Seidelhuber Metal Products, Inc.

            - Tru-Weld.

            - McNichols Co.

      - FERROUS METALS

        - Steel Plates, Shapes, and Bars:  ASTM A 36/A 36M.

        - Wire Rod for Grating Crossbars:  ASTM A 510 (ASTM A 510M).

      - FASTENERS

        - Steel Bolts and Nuts:  Regular hexagon-head bolts, ASTM A 307, Grade A (ASTM F 568M, Property Class 4.6); with hex nuts, ASTM A 563 (ASTM A 563M); and, where indicated, flat washers.  Bolts, nuts and washers to be hot dipped galvanized ASTM A153A/153M, Grade C.

        - Plain Washers:  Round, ASME B18.22.1 (ASME B18.22M).

        - Lock Washers:  Helical, spring type, ASME B18.21.1 (ASME B18.21.2M).

      - MISCELLANEOUS MATERIALS

        - Welding Rods and Bare Electrodes:  Select according to AWS specifications for metal alloy that is welded.

        - Galvanizing Repair Paint:  High-zinc-dust-content paint for regalvanizing welds in steel, complying with SSPC-Paint 20.

      - FABRICATION

        - Shop Assembly:  Fabricate grating sections in shop to greatest extent possible to minimize field splicing and assembly.  Disassemble units only as necessary for shipping and handling limitations.  Use connections that maintain structural value of joined pieces.  Clearly mark units for reassembly and coordinated installation.

        - Cut, drill, and punch material cleanly and accurately.  Remove burrs and ease edges to a radius of approximately 1/32 inch (1 mm), unless otherwise indicated.  Remove sharp or rough areas on exposed surfaces.

        - Form from materials of size, thickness, and shapes indicated, but not less than that needed to support indicated loads.

        - Fit exposed connections accurately together to form hairline joints.

        - Welding:  Comply with AWS recommendations and the following:

          - Use materials and methods that minimize distortion and develop strength and corrosion resistance of base metals.

          - Obtain fusion without undercut or overlap.

          - Remove welding flux immediately.

        - Provide for anchorage of type indicated; coordinate with supporting structure.  Fabricate and space the anchoring devices to secure gratings, frames, and supports rigidly in place and to support indicated loads.

          - Fabricate toeplates to fit grating units and weld to units in shop, unless otherwise indicated.

          - Toeplate Height:  as indicated.

      - METAL BAR GRATINGS

        - Welded Steel Grating :

          - Bearing Bar Spacing:  as indicated.

          - Bearing Bar Depth:  as indicated

          - Bearing Bar Thickness:  as indicated

          - Crossbar Spacing:  4 inches (102 mm) o.c.

          - Steel Finish:  Hot-dip galvanized with a coating weight of not less than 1.8 oz./sq. ft. (550 g/sq. m) of coated surface.

        - Removable Grating Sections:  Fabricate with banding bars attached by welding to entire perimeter of each section.  Include anchors and fasteners of type indicated or, if not indicated, as recommended by manufacturer for attaching to supports.

          - Provide not less than 4 saddle clips for each grating section composed of rectangular bearing bars 3/16 inch (4.8 mm) or less in thickness and spaced 15/16 inch (24 mm) or more o.c., with each clip designed and fabricated to fit over 2 bearing bars.

          - Furnish threaded bolts with nuts and washers for securing grating to supports.

        - Fabricate cutouts in grating sections for penetrations indicated.  Arrange cutouts to permit grating removal without disturbing items penetrating gratings.

          - Edge-band openings in grating that interrupt four or more bearing bars with bars of same size and material as bearing bars.

        - Do not notch bearing bars at supports to maintain elevation.

      - GRATING FRAMES AND SUPPORTS

        - Frames and Supports for Metal Gratings:  Fabricate from metal shapes, plates, and bars of welded construction to sizes, shapes, and profiles indicated and as necessary to receive gratings.  Miter and weld connections for perimeter angle frames.  Cut, drill, and tap units to receive hardware and similar items.

          - Unless otherwise indicated, fabricate from same basic metal as gratings.

        - Galvanize steel frames and supports.

      - STEEL FINISHES

        - Comply with NAAMM's "Metal Finishes Manual for Architectural and Metal Products" for recommendations for applying and designating finishes.

        - Finish gratings, frames, and supports after assembly.

        - Galvanizing:  For those items indicated for galvanizing, apply zinc coating by the hot-dip process complying with ASTM A 123/A 123M.

- EXECUTION

      - INSTALLATION, GENERAL

        - Fastening to In-Place Construction:  Provide anchorage devices and fasteners where necessary for securing gratings to in-place construction.

        - Cutting, Fitting, and Placement:  Perform cutting, drilling, and fitting required for installing gratings.  Set units accurately in location, alignment, and elevation; measured from established lines and levels and free of rack.

        - Fit exposed connections accurately together to form hairline joints.

          - Weld connections that are not to be left as exposed joints but cannot be shop welded because of shipping size limitations.  Do not weld, cut, or abrade the surfaces of exterior units that have been hot-dip galvanized after fabrication and are for bolted or screwed field connections.

        - Attach toeplates to gratings by welding at locations indicated.

        - Field Welding:  Comply with the following requirements:

          - Use materials and methods that minimize distortion and develop strength and corrosion resistance of base metals.

          - Obtain fusion without undercut or overlap.

          - Remove welding flux immediately.

      - INSTALLING METAL BAR GRATINGS

        - General:  Install gratings to comply with recommendations of referenced metal bar grating standards that apply to grating types and bar sizes indicated, including installation clearances and standard anchoring details.

        - Attach removable units to supporting members with type and size of clips and fasteners indicated or, if not indicated, as recommended by grating manufacturer for type of installation conditions shown.

      - ADJUSTING AND CLEANING

        - Galvanized Surfaces:  Clean field welds, bolted connections, and abraded areas and repair galvanizing to comply with ASTM A780.

END OF SECTION 055300