SECTION 05120

STRUCTURAL STEEL

- GENERAL

      - RELATED DOCUMENTS

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 1 Specification Sections, apply to this Section.

      - SUMMARY

        - This Section includes the following:

          - Structural steel.

          - Architecturally exposed structural steel.

          - Grout.

        - Related Sections include the following:

          - Division 1 Section "Quality Requirements" for independent testing agency procedures and administrative requirements.

          - Division 5 Section "Metal Fabrications" for miscellaneous steel fabrications and other metal items not defined as structural steel.

          - Division 9 painting Sections for surface preparation and priming requirements.

      - DEFINITIONS

        - Structural Steel:  Elements of structural-steel frame, as classified by AISC's "Code of Standard Practice for Steel Buildings and Bridges," that support design loads.

        - Architecturally Exposed Structural Steel:  Structural steel designated as architecturally exposed structural steel in the Contract Documents.

      - SUBMITTALS

        - Product Data:  For each type of product indicated.

        - Shop Drawings:  Show fabrication of structural-steel components.

          - Include details of cuts, connections, splices, camber, holes, and other pertinent data.

          - Include embedment drawings.

          - Indicate welds by standard AWS symbols, distinguishing between shop and field welds, and show size, length, and type of each weld.

          - Indicate type, size, and length of bolts, distinguishing between shop and field bolts.  Identify pre-tensioned and slip-critical high-strength bolted connections.

          - NO STRUCTURAL DRAWINGS IN ANY FORM SHALL BE USED AS A BACKGROUND FOR SHOP DRAWINGS AND ERECTION DRAWINGS.

          - CONTRACTOR SHALL VERIFY AND BECOME RESPONSIBLE FOR CORRECTNESS OF OTHER THAN PRINCIPAL CONTROLLING DIMENSIONS SHOWN ON THE CONTRACT DRAWINGS, AND CALL TO THE ATTENTION OF THE CONTRACTING OFFICER ANY ERRORS OR DISCREPANCIES THAT MAY BE DISCOVERED THEREIN.

        - Welding certificates.

        - Qualification Data:  For Installer and fabricator.

        - Mill Test Reports:  Signed by manufacturers certifying that the following products comply with requirements:

          - Structural steel including chemical and physical properties.

          - Bolts, nuts, and washers including mechanical properties and chemical analysis.

        - Source quality-control test reports.

      - QUALITY ASSURANCE

        - Installer Qualifications:  A qualified installer who participates in a quality control program.

        - Fabricator Qualifications:  A qualified fabricator who participates in a quality control program.

        - Welding:  Qualify procedures and personnel according to AWS D1.1, "Structural Welding Code--Steel."

        - Comply with applicable provisions of the following specifications and documents:

          - AISC's "Code of Standard Practice for Steel Buildings and Bridges."

          - AISC's "Seismic Provisions for Structural Steel Buildings" and "Supplement No. 2."

          - AISC's "Specification for Structural Steel Buildings--Allowable Stress Design and Plastic Design."

          - AISC's "Specification for the Design of Steel Hollow Structural Sections."

          - RCSC's "Specification for Structural Joints Using ASTM A325 or A490 Bolts."

        - Mockups:  Build mockups of architecturally exposed structural steel to set quality standards for fabrication and installation.

          - Coordinate finish painting requirements with Division 9 painting Sections.

          - Approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

        - Preinstallation Conference:  Conduct conference at Project site to comply with requirements in Division 1 Section "Project Management and Coordination."

      - DELIVERY, STORAGE, AND HANDLING

        - Store materials to permit easy access for inspection and identification.  Keep steel members off ground and spaced by using pallets, dunnage, or other supports and spacers.  Protect steel members and packaged materials from erosion and deterioration.

          - Store fasteners in a protected place.  Clean and relubricate bolts and nuts that become dry or rusty before use.

          - Do not store materials on structure in a manner that might cause distortion, damage, or overload to members or supporting structures.  Repair or replace damaged materials or structures as directed.

      - COORDINATION

        - Furnish anchorage items to be embedded in or attached to other construction without delaying the Work.  Provide setting diagrams, sheet metal templates, instructions, and directions for installation.

- PRODUCTS

      - STRUCTURAL-STEEL MATERIALS

        - W-Shapes:  ASTM A588/A588M, Grade 50.

        - Channels and Angles:  ASTM A 588/A 588M.

        - Channels and Angles to be painted: ASTM A36/ASTM A36M

        - Plate and Bar:  ASTM A588/A588M.

        - Cold-Formed Hollow Structural Sections: ASTM A500, Grade B, structural tubing.

        - Steel Pipe:  ASTM A53/A53M, Type E or S, Grade B.

          - Weight Class:  as indicated

          - Finish:  Black, except where indicated to be galvanized.

        - Medium-Strength Steel Castings:  ASTM A 27/A 27M, Grade 65-35 (Grade 450-240), carbon steel.

        - Welding Electrodes:  Comply with AWS requirements.

      - BOLTS, CONNECTORS, AND ANCHORS

        - High-Strength Bolts, Nuts, and Washers:  ASTM A 325 (ASTM A 325M), Type 1, heavy hex steel structural bolts; ASTM A 563 (ASTM A 563M) heavy hex carbon-steel nuts; and ASTM F 436 (ASTM F 436M) hardened carbon-steel washers.

          - Finish:  Corrosion Resistant.

        - Headed Anchor Rods:  ASTM A 307, Grade A (ASTM F 568M, Property Class 4.6), straight.

          - Nuts:  ASTM A 563 (ASTM A 563M) heavy hex carbon steel.

          - Plate Washers:  ASTM A 36/A 36M carbon steel.

          - Washers:  ASTM F 436 (ASTM F 436M) hardened carbon steel.

          - Finish:  Galvanized.

        - Threaded Rods:  ASTM A 36/A 36M.

          - Nuts:  ASTM A 563 (ASTM A 563M) heavy hex carbon steel.

          - Washers:  ASTM F 436 (ASTM F 436M) hardened carbon steel.

          - Finish:  Galvanized.

      - PRIMER

        - Primer:  Fabricator's standard lead- and chromate-free, nonasphaltic, rust-inhibiting primer.

      - GROUT

        - Cement Grout:  Portland cement, ASTM C 150, Type I; and clean, natural sand, ASTM C 404, Size No. 2.  Mix at ratio of 1 part cement to 2-1/2 parts sand, by volume, with minimum water required for placement and hydration.

        - Nonmetallic, Shrinkage-Resistant Grout:  ASTM C 1107, factory-packaged, nonmetallic aggregate grout, noncorrosive, nonstaining, mixed with water to consistency suitable for application and a 30-minute working time.

      - FABRICATION

        - Structural Steel:  Fabricate and assemble in shop to greatest extent possible.  Fabricate according to AISC's "Code of Standard Practice for Steel Buildings and Bridges" and AISC's "Specification for Structural Steel Buildings--Allowable Stress Design and Plastic Design."

          - Camber structural-steel members only where indicated.

          - Identify high-strength structural steel according to ASTM A 6/ A 6M and maintain markings until structural steel has been erected.

          - Mark and match-mark materials for field assembly.

          - Complete structural-steel assemblies, including welding of units, before starting shop-priming operations.

        - Architecturally Exposed Structural Steel:  Comply with fabrication requirements, including tolerance limits, of AISC's "Code of Standard Practice for Steel Buildings and Bridges" for structural steel identified as architecturally exposed structural steel.

          - Fabricate with exposed surfaces smooth, square, and free of surface blemishes including pitting, rust, scale and roughness.

          - Remove blemishes by filling or grinding or by welding and grinding, before cleaning, treating, and shop priming.

        - Thermal Cutting:  Perform thermal cutting by machine to greatest extent possible.

          - Plane thermally cut edges to be welded to comply with requirements in AWS D1.1.

        - Bolt Holes:  Cut, drill or punch standard bolt holes perpendicular to metal surfaces.

        - Weep Holes: Cut, drill or punch standard 1/8” diameter weep holes perpendicular to metal surfaces at all closed sections.

        - Finishing:  Accurately finish ends of columns and other members transmitting bearing loads.

        - Cleaning:  Clean and prepare steel surfaces that are to remain unpainted according to fabricator’s standard practice.

        - Holes:  Provide holes required for securing other work to structural steel and for passage of other work through steel framing members.

          - Cut, drill, or punch holes perpendicular to steel surfaces. Do not thermally cut bolt holes or enlarge holes by burning.

          - Base-Plate Holes:  Cut, drill, mechanically thermal cut, or punch holes perpendicular to steel surfaces.

          - Weld threaded nuts to framing and other specialty items indicated to receive other work.

      - SHOP CONNECTIONS

        - High-Strength Bolts:  Shop install high-strength bolts according to RCSC's "Specification for Structural Joints Using ASTM A 325 or A 490 Bolts" for type of bolt and type of joint specified.

          - Joint Type:  Snug tightened.

        - Weld Connections:  Comply with AWS D1.1 for welding procedure specifications, tolerances, appearance, and quality of welds and for methods used in correcting welding work.

          - Remove backing bars or runoff tabs, back gouge, and grind steel smooth.

          - Assemble and weld built-up sections by methods that will maintain true alignment of axes without exceeding tolerances of AISC's "Code of Standard Practice for Steel Buildings and Bridges" for mill material.

          - Verify that weld sizes, fabrication sequence, and equipment used for architecturally exposed structural steel will limit distortions to allowable tolerances.  Prevent weld show-through on exposed steel surfaces.

      - SHOP PRIMING

        - Shop prime steel surfaces except the following:

          - Surfaces embedded in concrete or mortar.  Extend priming of partially embedded members to a depth of 2 inches (50 mm).

          - Surfaces to be field welded.

          - Galvanized surfaces.

          - Corrosion Resistant shapes.

        - Surface Preparation:  Clean surfaces to be painted.  Remove loose rust and mill scale and spatter, slag, or flux deposits.  Prepare surfaces according to the following specifications and standards:

          - SSPC-SP 2, "Hand Tool Cleaning" or SSPC-SP3, “Power Tool Cleaning”

        - Priming:  Immediately after surface preparation, apply primer according to manufacturer's written instructions and at rate recommended by SSPC to provide a dry film thickness of not less than 1.5 mils (0.038 mm).  Use priming methods that result in full coverage of joints, corners, edges, and exposed surfaces.

          - Stripe paint corners, crevices, bolts, welds, and sharp edges.

          - Apply two coats of shop paint to inaccessible surfaces after assembly or erection.  Change color of second coat to distinguish it from first.

      - SOURCE QUALITY CONTROL

        - Engage an independent testing and inspecting agency to perform shop tests and inspections and prepare test reports.

          - Provide testing agency with access to places where structural-steel work is being fabricated or produced to perform tests and inspections.

        - Correct deficiencies in Work that test reports and inspections indicate does not comply with the Contract Documents.

        - Bolted Connections:  Shop-bolted connections may be inspected according to RCSC's "Specification for Structural Joints Using ASTM A 325 or A 490 Bolts."

        - Welded Connections:  In addition to visual inspection, shop-welded connections may be tested and inspected according to AWS D1.1 and the following inspection procedures, at testing agency's option:

          - Liquid Penetrant Inspection:  ASTM E 165.

          - Magnetic Particle Inspection:  ASTM E 709; performed on root pass and on finished weld.  Cracks or zones of incomplete fusion or penetration will not be accepted.

          - Ultrasonic Inspection:  ASTM E 164.

          - Radiographic Inspection:  ASTM E 94.

- EXECUTION

      - EXAMINATION

        - Verify elevations of concrete- bearing surfaces and locations of anchor rods, bearing plates, and other embedments, with steel erector present, for compliance with requirements.

        - Proceed with installation only after unsatisfactory conditions have been corrected.

      - PREPARATION

        - Provide temporary shores, guys, braces, and other supports during erection to keep structural steel secure, plumb, and in alignment against temporary construction loads and loads equal in intensity to design loads.  Remove temporary supports when permanent structural steel, connections, and bracing are in place, unless otherwise indicated.

      - ERECTION

        - Set structural steel accurately in locations and to elevations indicated and according to AISC's "Code of Standard Practice for Steel Buildings and Bridges" and "Specification for Structural Steel Buildings--Allowable Stress Design and Plastic Design."

        - Base and Bearing Plates:  Clean concrete-bearing surfaces of bond-reducing materials, and roughen surfaces prior to setting base and bearing plates.  Clean bottom surface of base and bearing plates.

          - Set base and bearing plates for structural members on wedges, shims, or setting nuts as required.

          - Weld plate washers if indicated to top of base plate.

          - Snug-tighten anchor rods after supported members have been positioned and plumbed.  Do not remove wedges or shims but, if protruding, cut off flush with edge of base or bearing plate before packing with grout.

          - Promptly pack grout solidly between bearing surfaces and base or bearing plates so no voids remain.  Neatly finish exposed surfaces; protect grout and allow to cure. Comply with manufacturer's written installation instructions for shrinkage-resistant grouts.

        - Maintain erection tolerances of structural steel and architecturally exposed structural steel within AISC's "Code of Standard Practice for Steel Buildings and Bridges."

        - Align and adjust various members forming part of complete frame or structure before permanently fastening.  Before assembly, clean bearing surfaces and other surfaces that will be in permanent contact with members.  Perform necessary adjustments to compensate for discrepancies in elevations and alignment.

          - Level and plumb individual members of structure.

          - Make allowances for difference between temperature at time of erection and mean temperature when structure is completed and in service.

        - Splice members only where indicated.

        - Remove erection bolts on welded, architecturally exposed structural steel; fill holes with plug welds; and grind smooth at exposed surfaces.

        - Do not use thermal cutting during erection.

        - Do not enlarge unfair holes in members by burning or using drift pins.  Ream holes that must be enlarged to admit bolts.

      - FIELD CONNECTIONS

        - High-Strength Bolts:  Install high-strength bolts according to RCSC's "Specification for Structural Joints Using ASTM A 325 or A 490 Bolts" for type of bolt and type of joint specified.

          - Joint Type:  Snug tightened.

        - Weld Connections:  Comply with AWS D1.1 for welding procedure specifications, tolerances, appearance, and quality of welds and for methods used in correcting welding work.

          - Comply with AISC's "Code of Standard Practice for Steel Buildings and Bridges" and "Specification for Structural Steel Buildings--Allowable Stress Design and Plastic Design" for bearing, adequacy of temporary connections, alignment, and removal of paint on surfaces adjacent to field welds.

          - Remove backing bars or runoff tabs, back gouge, and grind steel smooth.

          - Assemble and weld built-up sections by methods that will maintain true alignment of axes without exceeding tolerances of AISC's "Code of Standard Practice for Steel Buildings and Bridges" for mill material.

          - Verify that weld sizes, fabrication sequence, and equipment used for architecturally exposed structural steel will limit distortions to allowable tolerances.

      - FIELD QUALITY CONTROL

        - Testing Agency:  Contractor will engage a qualified independent testing and inspecting agency to inspect field welds and high-strength bolted connections.

        - Bolted Connections:  Shop-bolted and field-bolted connections may be field tested and inspected according to RCSC's "Specification for Structural Joints Using ASTM A 325 or A 490 Bolts."

        - Welded Connections:  Field welds will be visually inspected according to AWS D1.1.

          - In addition to visual inspection, field welds may be tested according to AWS D1.1 and the following inspection procedures, at testing agency's option:

            - Liquid Penetrant Inspection:  ASTM E 165.

            - Magnetic Particle Inspection:  ASTM E 709; performed on root pass and on finished weld.  Cracks or zones of incomplete fusion or penetration will not be accepted.

            - Ultrasonic Inspection:  ASTM E 164.

            - Radiographic Inspection:  ASTM E 94.

        - Correct deficiencies in Work that test reports and inspections indicate does not comply with the Contract Documents.

      - REPAIRS AND PROTECTION

        - Repair damaged galvanized coatings on galvanized items with galvanized repair paint according to ASTM A 780 and manufacturer's written instructions.

        - Touchup Priming:  After installation, promptly clean, prepare, and prime or reprime field connections, rust spots, and abraded surfaces of prime-painted accessories, bearing plates, and abutting structural steel.

          - Clean and prepare surfaces by SSPC-SP 2 hand-tool cleaning or SSPC-SP 3 power-tool cleaning.

          - Apply a compatible primer of same type as shop primer used on adjacent surfaces.

        - Touchup Painting:  Cleaning and touchup painting are specified in Division 9 painting Sections.

END OF SECTION 05120