SECTION 09912

EXTERIOR PAINTING

- GENERAL

      - RELATED DOCUMENTS

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

      - SUMMARY

        - This Section includes surface preparation and the application of paint systems on the following exterior substrates:

          - Steel.

        - Related Sections include the following:

          - Division 05 Sections for shop priming of metal substrates with primers specified in this Section.

      - SUBMITTALS

        - Product Data:  For each type of product indicated.

        - Samples for Initial Selection:  For each type of topcoat product indicated.

        - Samples for Verification:  For each type of paint system and each color and gloss of topcoat indicated.

          - Submit Samples on rigid backing, 8 inches (200 mm) square.

          - Step coats on Samples to show each coat required for system.

          - Label each coat of each Sample.

          - Label each Sample for location and application area.

        - Product List:  For each product indicated, include the following:

          - Cross-reference to paint system and locations of application areas.  Use same designations indicated on Drawings and in schedules.

          - Printout of current "MPI Approved Products List" for each product category specified in Part 2, with the proposed product highlighted.

      - QUALITY ASSURANCE

        - MPI Standards:

          - Products:  Complying with MPI standards indicated and listed in "MPI Approved Products List."

          - Preparation and Workmanship:  Comply with requirements in "MPI Architectural Painting Specification Manual" for products and paint systems indicated.

        - Mockups:  Apply benchmark samples of each paint system indicated and each color and finish selected to verify preliminary selections made under sample submittals and to demonstrate aesthetic effects and set quality standards for materials and execution.

          - Contracting Officer will select one surface to represent surfaces and conditions for application of each paint system specified in Part 3.

            - Vertical and Horizontal Surfaces:  Provide samples of at least 100 sq. ft. (9 sq. m).

            - Other Items:  Contracting Officer will designate items or areas required.

          - Final approval of color selections will be based on benchmark samples.

            - If preliminary color selections are not approved, apply additional benchmark samples of additional colors selected by Contracting Officer at no added cost to Owner.

      - DELIVERY, STORAGE, AND HANDLING

        - Store materials not in use in tightly covered containers in well-ventilated areas with ambient temperatures continuously maintained at not less than 45 deg F (7 deg C).

          - Maintain containers in clean condition, free of foreign materials and residue.

          - Remove rags and waste from storage areas daily.

      - PROJECT CONDITIONS

        - Apply paints only when temperature of surfaces to be painted and ambient air temperatures are between 50 and 95 deg F (10 and 35 deg C).

        - Do not apply paints in snow, rain, fog, or mist; when relative humidity exceeds 85 percent; at temperatures less than 5 deg F (3 deg C) above the dew point; or to damp or wet surfaces.

      - EXTRA MATERIALS

        - Furnish extra materials described below that are from same production run (batch mix) as materials applied and that are packaged for storage and identified with labels describing contents.

          - Quantity:  Furnish an additional 5 percent, but not less than 1 gal. (3.8 L) of each material and color applied.

- PRODUCTS

      - MANUFACTURERS

        - Available Manufacturers:  Subject to compliance with requirements, manufacturers offering products that may be incorporated into the Work include, but are not limited to, the following:

          - Benjamin Moore & Co.

          - Benjamin Moore & Co., Limited (Canada).

          - Bennette Paint Mfg. Co., Inc.

          - BLP Mobile Paint Manufacturing.

          - California Paints.

          - Cloverdale Paint.

          - Color Wheel Paints & Coatings.

          - Columbia Paint & Coatings.

          - Coronado Paint.

          - Davis Paint Company.

          - Del Technical Coatings.

          - Diamond Vogel Paints.

          - Dunn-Edwards Corporation.

          - Durant Paints Inc.

          - Duron, Inc.

          - Envirocoat Technologies Inc.

          - Farrell-Calhoun.

          - Flex Bon Paints.

          - Frazee Paint.

          - General Paint.

          - Griggs Paint.

          - Hallman Lindsay Quality Paints.

          - Hirshfield's, Inc.

          - ICI Devoe (Canada).

          - ICI Paints.

          - ICI Paints (Canada).

          - Insl-x.

          - Iowa Paint Manufacturing Company, Inc.

          - Kelly-Moore Paints.

          - Kwal-Howells Paint.

          - M.A.B. Paints.

          - McCormick Paints.

          - Miller Paint.

          - Mills Paint.

          - NCP Coatings.

          - Northern Paint.

          - PARA Paints.

          - Parker Paint Mfg. Co. Inc.

          - Porter Paints.

          - PPG Contracting Officerural Finishes, Inc.

          - Rodda Paint Co.

          - Sherwin-Williams Company (The).

          - Sico, Inc.

          - Sigma Coatings.

          - Smiland Paint Company.

          - Spectra-Tone.

          - Tamms Industries, Inc.

          - Tower Paint.

          - Vista Paint.

      - PAINT, GENERAL

        - Material Compatibility:

          - Provide materials for use within each paint system that are compatible with one another and substrates indicated, under conditions of service and application as demonstrated by manufacturer, based on testing and field experience.

          - For each coat in a paint system, provide products recommended in writing by manufacturers of topcoat for use in paint system and on substrate indicated.

        - Colors:  Black

      - METAL PRIMERS

        - Alkyd Anticorrosive Metal Primer:  MPI #79.

          - VOC Content:  E Range of [E1] [E2].

        - Quick-Drying Alkyd Metal Primer:  MPI #76.

          - VOC Content:  E Range of [E1] [E2] [E3].

        - Cementitious Galvanized-Metal Primer:  MPI #26.

          - VOC Content:  E Range of E1.

        - Waterborne Galvanized-Metal Primer:  MPI #134.

          - VOC Content:  E Range of [E1] [E2] [E3].

          - Environmental Performance Rating:  [EPR 1] [EPR 2] [EPR 3].

      - EXTERIOR LATEX PAINTS

        - Exterior Latex (Flat):  MPI #10 (Gloss Level 1).

          - VOC Content:  E Range of [E1] [E2] [E3].

        - Exterior Latex (Semigloss):  MPI #11 (Gloss Level 5).

          - VOC Content:  E Range of [E1] [E2] [E3].

        - Exterior Latex (Gloss):  MPI #119 (Gloss Level 6, except minimum gloss of 65 units at 60 deg).

          - VOC Content:  E Range of [E1] [E2] [E3].

      - EXTERIOR ALKYD PAINTS

        - Exterior Alkyd Enamel (Flat):  MPI #8 (Gloss Level 1).

          - VOC Content:  E Range of E1.

        - Exterior Alkyd Enamel (Semigloss):  MPI #94 (Gloss Level 5).

          - VOC Content:  E Range of [E1] [E2].

        - Exterior Alkyd Enamel (Gloss):  MPI #9 (Gloss Level 6).

          - VOC Content:  E Range of [E1] [E2].

- EXECUTION

      - EXAMINATION

        - Examine substrates and conditions, with Applicator present, for compliance with requirements for maximum moisture content and other conditions affecting performance of work.

        - Verify suitability of substrates, including surface conditions and compatibility with existing finishes and primers.

        - Begin coating application only after unsatisfactory conditions have been corrected and surfaces are dry.

          - Beginning coating application constitutes Contractor's acceptance of substrates and conditions.

      - PREPARATION

        - Comply with manufacturer's written instructions and recommendations in "MPI Architectural Painting Specification Manual" applicable to substrates and paint systems indicated.

        - Remove plates, machined surfaces, and similar items already in place that are not to be painted.  If removal is impractical or impossible because of size or weight of item, provide surface-applied protection before surface preparation and painting.

          - After completing painting operations, use workers skilled in the trades involved to reinstall items that were removed.  Remove surface-applied protection if any.

          - Do not paint over labels of independent testing agencies or equipment name, identification, performance rating, or nomenclature plates.

        - Clean substrates of substances that could impair bond of paints, including dirt, oil, grease, and incompatible paints and encapsulants.

          - Remove incompatible primers and reprime substrate with compatible primers as required to produce paint systems indicated.

      - APPLICATION

        - Apply paints according to manufacturer's written instructions.

          - Use applicators and techniques suited for paint and substrate indicated.

          - Paint surfaces behind movable items same as similar exposed surfaces.  Before final installation, paint surfaces behind permanently fixed items with prime coat only.

        - Tint each undercoat a lighter shade to facilitate identification of each coat if multiple coats of same material are to be applied.  Tint undercoats to match color of topcoat, but provide sufficient difference in shade of undercoats to distinguish each separate coat.

        - If undercoats or other conditions show through topcoat, apply additional coats until cured film has a uniform paint finish, color, and appearance.

        - Apply paints to produce surface films without cloudiness, spotting, holidays, laps, brush marks, roller tracking, runs, sags, ropiness, or other surface imperfections.  Cut in sharp lines and color breaks.

      - FIELD QUALITY CONTROL

        - Testing of Paint Materials:  Owner reserves the right to invoke the following procedure at any time and as often as Owner deems necessary during the period when paints are being applied:

          - Owner will engage the services of a qualified testing agency to sample paint materials being used.  Samples of material delivered to Project site will be taken, identified, sealed, and certified in presence of Contractor.

          - Testing agency will perform tests for compliance of paint materials with product requirements.

          - Owner may direct Contractor to stop applying paints if test results show materials being used do not comply with product requirements.  Contractor shall remove noncomplying-paint materials from Project site, pay for testing, and repaint surfaces painted with rejected materials.  Contractor will be required to remove rejected materials from previously painted surfaces if, on repainting with complying materials, the two paints are incompatible.

      - CLEANING AND PROTECTION

        - At end of each workday, remove rubbish, empty cans, rags, and other discarded materials from Project site.

        - After completing paint application, clean spattered surfaces.  Remove spattered paints by washing, scraping, or other methods.  Do not scratch or damage adjacent finished surfaces.

        - Protect work of other trades against damage from paint application.  Correct damage to work of other trades by cleaning, repairing, replacing, and refinishing, as approved by Contracting Officer, and leave in an undamaged condition.

        - At completion of construction activities of other trades, touch up and restore damaged or defaced painted surfaces.

      - EXTERIOR PAINTING SCHEDULE

        - Steel Substrates:

          - Quick-Drying Enamel System:  MPI EXT 5.1A.

            - Prime Coat:  Quick-drying alkyd metal primer.

            - Intermediate Coat:  Quick-drying enamel matching topcoat.

            - Topcoat:  Quick-drying enamel [(semigloss)] [(high gloss)].

          - Alkyd System:  MPI EXT 5.1D.

            - Prime Coat:  Alkyd anticorrosive metal primer.

            - Intermediate Coat:  Exterior alkyd enamel matching topcoat.

            - Topcoat:  Exterior alkyd enamel [(flat)] [(semigloss)] [(gloss)].

          - Aluminum Paint System:  MPI EXT 5.1K.

            - Prime Coat:  Alkyd anticorrosive metal primer.

            - Intermediate Coat:  Aluminum paint.

            - Topcoat:  Aluminum paint.

END OF SECTION 099113